SYNG-2 PROTOTYPE AND CHARACTERISATION OF THE NEXT GENERATION OF GNSS RF DOWN-CONVERTER ASIC
DiReRa
New Rad-Hard Chip-Set
for Radiometers
AMICSA 2016
[Speaker Notes: Page Page Page]

---
PowerPoint Presentation
Outline
Radiometer Architecture
Requirements and Frequency Plans
IC Process Constraints and Requirements
DiReRa Chip-Set: RF Front-End
DiReRa Chip-Set: AD-Converter
Measurement Results
Radiation Hardening – TID
Radiation Hardening – Heavy Ions
Conclusions and Road Map
[Speaker Notes: Page Page Page]

---
Radiometer Architecture
Full H-V polarimetric radiometer – TRYO Aerospace.
Measures both H and V polarizations at the same time.
DiReRa chip-set is shown in orange. It consists of:
→ L-band RF front-end.
→ Dual-channel 1-bit AD-converter (comparator).

---
Requirements, Frequency Plans
IC – Reduce size and power consumption considerably.
Maintain compatibility with existing LICEF-3 radiometer.
Isolation between channels is critical.
RF bandwidth = 20MHz, flatness = ± 0.1-0.2dB.
Support different frequency plans.
No.	RF Frequency	LO Frequency	IF Frequency	Sampling Freq.	Note
1	1200-1600 MHz	1180-1580 MHz	25-35 MHz	130 MHz	ESA SoW.
2	1413.5 MHz	1396 MHz	17.5 MHz	55.84 MHz	TA – LICEF-3.
3	1413.5MHz	1384.65MHz	28.85MHz	115.38MHz	TA – SMOSops.
4	1200-1600 MHz	1167.5-1567.5 MHz	32.5 MHz	130 MHz	As 1, centered.
5	1200-1600 MHz	1037.5-1437.5 MHz	162.5 MHz	130 MHz	As 1, higher IF.
6	1413.6 MHz	1288 MHz	125.6 MHz	55.84 MHz	As 2, higher IF.
[Speaker Notes: Page Page Page]

---
IC Constraints and Requirements
Single process must fit everything.
Limited component types and values, large tolerances, but excellent component matching.
Coupling via common substrate and pins.
► Use differential
     signal paths.
Proper GHz RF performances (dominant requirement).
Rad-hard – can be radiation hardened.
Available in small quantities – a few 100 dies yearly.
► AMS S35 – 0.35µm HBT BiCMOS process.
Constraints
Requirem.

---
RF Downconverter ASIC
► Architecture
Single conversion superheterodyne, active mixer.
Balanced signal path (except LNA), 50Ω RF, 600Ω IF.
High Z local oscillator port
and good mixer isolation:
→ Bridging is possible.

---
RF Downconverter ASIC
► Layout and Test Fixture
Size: 1280μm x 1200μm.
42 pads, bonded to 40 pins.
QFN test plastic package.
JEDEC MO-220, VJJD-5

---
AD-Converter ASIC
► Architecture
Dual channel 1-bit AD-converter (dual comparator).
Latched regenerative architecture (high sens., low power).
0-1 imbalance ≤ 0.5%: critical.
Direct and muxed outputs with deglitching circuit
(compatible with existing LICEF-3 baseband processor).

---
AD-Converter ASIC
► Layout and Test Fixture
Size: 610μm x 880μm.
16 pads, bonded to 16 pins.
QFN test plastic package.
JEDEC MO-220, VGGC-2

---
Measured Results
Parameter	Conditions	Value	Unit	Notes
DiReRa RF Front-End
LNA gain	High gain setting	18.3	dB	Noise matched, 50Ω.
	Low gain setting	6.5	dB
LNA noise figure	High gain setting	1.7	dB	Noise matched, 50Ω.
	Low gain setting	2.3	dB
Mixer SSB voltage gain	Balanced input, 50Ω	14.7	dB	Balanced output, no load.
Mixer SSB noise figure		12.3	dB
IF-strip gain range	TIF output	23.5-81.6	dB	PGAs+VCA, balanced, no load.
IF-strip PGA gain step		1	dB	Balanced I/Os, no load.
IF-strip VCA gain range	VC=0V to 2V	12	dB	Maximum gain is limited.
Output 1dB compr. point	PNS output, no load	−4.5	dBu	Referred to 600Ω.
DADC 1-bit AD-converter
Sampling frequency	Maximum	130	MHz	Operates from ~0Hz to 130MHz.
DC-offset	Input referred	±3.7	mV	Measured at DC, 2 samples.
0-1 imbalance	−4dBu, −40 to 125°C	0.5	%	Band-limited AWGN.

---
Radiation Hardening – TID
► TOTAL DOSE – Objective: ≥ 1kGy(Si) [100krad(Si)].
► Effects – MOS: Vt shift, leakages; BJT: β degradation.
Strongly process dependent, no way to predict ELDRS.
But – AMS S35 is already well tested (SY10x7 devices):
→ TD > 1kGy at 0.12Gy/min.
Some circuit/layout tricks:
→ Differential stages:
- Vgs shifts will compensate.
→ High current or active
bias circuits:
- Allow for β reduction.
→ Layout techniques.

---
Radiation Hardening – SEL
► HEAVY IONS – Objective: LET ≥ 85MeV∙cm²/mg.
SEL is potentially destructive. Some SEL-tolerant techniques:
Continuous uninterrupted guard rings.
Good distributed substrate/well contacts.
Silicon on Insulator (SOI) – but beware TID effects.
►SEL at LET < 60MeV∙cm²/mg requires SEL protection.
Latch-up circuit
SEL-tolerant layout example

---
Radiation Hardening – SET/SEU
SET/SEU cause noise (analog) or operating errors (digital) but are not destructive. SEE protection shall not compromise perf-ormance excessively! Some SEE-tolerant techniques are:
Drive strength hardening (DSH).
Error correction (ECC, TMR, DICE).
Glitch suppression, charge storage devices.
Self-resetting sequential circuits, no dead cycles.
Fast recovery analog circuits.
► DSH provides intrinsic protection, i.e. prevents SEE from occurring, but effectiveness is limited to ~5-15MeV∙cm²/mg.
► The other methods don't prevent SEE but only correct its effects. LET ≥ 85MeV∙cm²/mg can be achieved with ECC or TMR, DICE is ~30-50MeV∙cm²/mg (on 0.35μm process).

---
Conclusions, Road Map
The DiReRa chip-set has been designed, manufactured and tested with good results, now it should be industrialized:
Do a preliminary irradiation test on current prototypes.
Finalize design, do an engineering run.
Procure and assemble the packages.
Develop production screening.
Do a qualification of the chip-set.
Prepare all needed documentation.
Once these steps are completed the chip-set is ready to be used in a radiometer and will be introduced in Saphyrion's catalogue.

---
Thank you for your attention
[Speaker Notes: Page Page Page]