## Slide 1
Optimizing Ge substrate usage in the manufacturing of MJ solar cells
Guillaume Courtois, Valerie De Houwer, Jinyoun Cho, Kristof Dessein
Notes: Until it found its way into MJ solar cells. These solar cells were historically produced on GaAs substrates, but in the early 1990s, germanium pushed those out completely. Why is that?

## Slide 2: Outline
Ge substrates for multi-junction solar cells
  Sourcing
  Recycling of losses incurred at Umicore
Substrates thinning down at end-of-line
  Recycling of Ge losses incurred at a customer’s
Future thin Ge substrates
  Just as enough Ge as needed in solar cells
ESA Projects
Effective Use of Ge*
ELLA+
*Contract 4000128156/19/NL/FE
+Contract 4000129924/20/NL/FE
GaInP
GaAs
Ge

## Slide 3: 1. Ge substrates for MJ solar cells

## Slide 4: Germanium Solutions
GeCl4
High Purity Germanium
Germanium Sourcing & Supply
Germanium Substrates
Germanium Recycling
Germanium
Solutions
Production scraps & EoLife products
Sustainable closed-loop model

## Slide 5: Germanium sources
Chart: 
| Coal | Zinc | Other
Chart tile | 56 | 33 | 11
Global market is 120 – 150 tons per year
Chart: 
| Secondary (recycled) | Primary
Source | 55 | 45
Global Primary Germanium Sources
Umicore sourcing 2022
Robertz, B., Verhelle, J. & Schurmans, M. JOM67(2015) : 412

## Slide 6: Importance of germanium recycling
CO2 impact lower for entire production line
Win-win for customer & Umicore  insusceptible to germanium price fluctuations  lower end-product price
Germanium is included in list of EU’s Critical Raw Materials (CRM)

## Slide 7: Production scrap recycling
Study case: 100k wafers, Ø 150 mm, 225 µm delivered to customer, 145 µm after backgrinding
All Ge losses incurred in Umicore’s internal flow are recycled
New: Recycling of Ge losses incurred at customers’ being implemented
Recycled internally
Recovered at customers’
Space (30%)
Wafering
Umicore
Customers

## Slide 8: Motivation for back-grinding
Lighter cells, leaner in Ge
AzurSpace 3G30C GaInP/GaAs/Ge triple junction solar cells

## Slide 9: 2. Recycling of Ge losses incurred at customer’s

## Slide 10: Recycling Ge from End-of-Line back-grinding
Up-concentration needs to occur at the customer’s
Backgrinding
Ship grinding waters to Umicore
Storage
Backgrinding
Ship grinding waters to Umicore
Up-concentration
Backgrinding
Up-concentration at customer’s facility
Up-concentration
0 % Ge recovered (dissolved in water)
30 % Ge recovered (dissolved in water)
90 % Ge recovered (bench top setup)

## Slide 11: Summary of experimental work
Ge separation
Instability of solution over time
 Tests onsite necessary
Ge recovery > 80%
Optimization process parameters
Volume reduction of 98%
High concentration achieved
Stable operation
Long-term stable operation guaranteed
Lab trials @ Umicore
Lab trials @ Azur
Pilot trials @ Azur
Production run using pilot
Installation of final process
Successful commissioning of on-site upconcentration process
Successfully closed the loop starting from Azur’s material
New 2022!

## Slide 12: Scope of the LCA study
Functional unit = Manufacturing of one output 4” or 6” Ge wafer with back-grinding
Baseline scenario: no recycling

## Slide 13: Progress of the LCA study
Iteration 1
  Outcome: relative low climate change impact results compared to previous studies
   Include Umicore’s process data for primary Ge route (Zinc by-product)
Iteration 2 Outcome: wafer manufacturing + cleaning & inspection processes had relatively small contribution  Include Umicore’s process data for manufacturing + cleaning & inspection
Iteration 3 Outcome: updated LCI

## Slide 14: Back-grinding LCA: Results third iteration
2 scenarios:
  Baseline: back-grinding without recycling
  Back-grinding + Recycling
Recycling decreases:
  Climate change impact
  Primary energy usage
  Minerals & metals resource depletion
  Acidification
Recycling increases:
  Marine eutrophication
  Freshwater ecotoxicity
Due to hydrometallurgical recycling step
6” wafer: Comparison between baseline and recycling scenarios

## Slide 15: 3. Future thin Ge substrates

## Slide 16: How thick a Ge substate?
mechanical support (> 100 µm)
radiation shielding (> 20 µm)
functionality for which Ge is indispensable
growth template (< 1µm)
bottom cell (< 10 µm)
functionality for which Ge is optional
Going for...
Lighter
Flexible
Cheaper
Ge substrates
Ge Epi layer, 10µm
Ge mother substrate

## Slide 17: Ge-on-Ge platform
Closing the loop
(1) Ge wafer
(6) Reconditioned Ge wafer
(2) Ge-on-Ge engineering
(3) Epitaxial thickening (optional)
(4) Device processing
(5) Layer transfer

## Slide 18: Ge-on-Ge wafers processed into 2J solar cells
Best Ref cell
Best Ge-on-Ge cell
6” wafers
n-type Ge  no bottom cell
Engineered: pores
  No risk of delamination
Standard ARC added
Reference cells: on standard wafer
Jsc on par with reference cell
Voc loss mostly explained by absence of Ge bottom cell
Normal FF
6”

## Slide 19: Ge-on-Ge foils surviving the full solar cell process
With comparable EQE as Ref cell
Ge-on-Ge wafers thickened with 7µm epiGe
GaInP/GaInAs/Ge TJ solar cells still attached
Ge
GaInAs
GaInP
Ga-doped Ge ~ 5E17/cm3
Ge-on-Ge + 7 µm epiGe
Plated Ti/Ni/Au
No ARC!
5.5 µm
7.5 µm
V. Depauw et al., Progress in PV (accepted)
Ref cell
Ge-on-Ge cells
Ge-on-Ge
~ 2.5 cm

## Slide 20: Ge-on-Ge engineered substrates: What’s next?
Need dedicated bonding/detachment process
Process and measure detached solar cells
The device detachment challenge
Triple-junction solar cell on Ge-on-Ge
Kapton tape
Glass slide
3-junction cell
Target

## Slide 21: Conclusion & Outlook
Present generation of substrates: Improve Ge recycling
  Back-grinding losses incurred @ AzurSpace fully recycled
  Similar request from other customers
  Towards 100% recycling of Ge production scraps
Reduce Ge usage in solar cells: Future, thin substrates
  10µm Ge foil for triple junction cells
  Ge consumption down to 130 mg/W
  Promising III-V stack quality and preliminary device results
  Challenge: Detachment of large area devices & back-side metallization

## Slide 22
Guillaume.Courtois@eu.umicore.com
We are hiring!
careers.umicore.com

## Slide 23: ESA Effective Use of Germanium
The work presented here was supported by the European Space Agency under the Effective Use of Germanium project
Project partners:
Key external service providers:
Key goals:
Recycling of backgrinding waters of Azur Space
Ge-on-Ge engineered substrates as alternative growth substrates
Contract number: 4000128156/19/NL/FE

## Slide 25: Batch 3
3G30 on 6” v1.1: cell results
Isc= nearly on target
Voc = difference due to lack of Ge bottom cell
FF = nearly on target
v1.0
v2.0
v3.0

## Slide 26: Ge lift-off techniques 2/2: Wet etching
Porous Ge: High-porosity PGe structure enable easy detachment
PGe substrate
Ge epilayer
Free-standing Ge membrane
Same Ge benefits Potential for low cost starting substrate, low cost and good re-usability potential
Early in development cycle
Mirror like surface, without any delaminations
High quality Epitaxial Ge with formation of weak layer
Low roughness (RMS ~1 nm)
Highly oriented monocrystalline nature of Ge membrane
Crack free surface Ge membrane
N. Paupy et al., IEEE-PVSC49 (2022)
T. Hanus et al., E-MRS Fall (2022)

## Slide 27
N. Paupy et al., 2022, submitted
4”, 145µm
5µm