## Slide 1: EXPERIMENTAL DEMISE STUDY OF NOVEL MATERIALS COMBINATIONS FOR SPACECRAFT STRUCTURAL PANEL ASSEMBLIES
A.A. Looten (EPFL), V. Michaud (EPFL), M. Richard (ClearSpace), A. Caiazzo (ESA)
ESA Clean Space Industry Days – 10 to 13 October 2022

## Slide 2: Uncontrolled reentry events
On-ground direct threat from planned or accidental uncontrolled reentering objects
Causes:
    Rising numbers of satellited objects, +400% in Q1 of 2022 compared to 2019
    Incomplete and inaccurate demise models for composite materials
    The use of of critically resistant materials for external panel and/or joining systems leading to shading and late demise exposure
Context
CFRP element remaining from Crew-1 capsule trunk reentry - Australia, July 2022
nzherald.co.nz
October 2021 over Michigan (USA) – Kosmos/2551 uncontrolled reentry
space.com
youtube.com/watch?v=s4x7Kcm8uj0
Multifactorial global risk
Ground impact probability is increasing everyday !
We need to act now to push for a sustainable space safety
Notes: Casualty risk

## Slide 3: D4D applied to S/C external sandwich panel
  Highest impact on demise depends on material selection and exposure altitude parameters, M.Trisolini et al. 2018 [2].
  Our project focus on material substitution of external panel by optimal demisable composite design
Project Goal
Improve overall S/C demisability by earlier demise/release of the external panels
Project Goal
[2] M.Trisolini et al. 2018, Demisability and survivability sensitivity to design-for-demise techniques
eoportal.org/satellite-missions/calipso#spacecraft
Notes: Out of the several mitigation approaches to this issue, we focused our research on the D4D one and more specifically on the material selection aspect
Which following a survivability and demisability sensitivity analysis by Trisolini et al. is the major parameter of influence as well as the break-up/altitude of demise on the timeline aspect.
Therefore we focused our project on material substitution applied to S/C structural panels and more specifically by optimal demisable composite design.
Today I will just talk about the fasteners chapter, which

## Slide 4: Novel composite design
Benchmark design = sandwich panel with through-thickness bolted joint insert system
Best Trade off between mechanical and demise performance
  Hybrid carbon + flax in a ply-by-ply configuration with AlMg µ-powder filled epoxy
  Short carbon fiber reinforced PEEK bolt
Sandwich panel skin
NEW DESIGNS
BASELINE
Aluminium
Al2024-T81
Carbon Fiber
Flax Fiber
CF/FF Tow-Tow
CF+FFP Ply-Ply
Reinforcement
Thermoset - Epoxy
Matrix
Blend thermoset/thermoplast
AlMg µ-powder
Reactive Filler
None
+
+
Hybrids
Dual Approach
Credits: RUAG Schweiz AG
Bolted fastener
Stainless steel
Ti-6Al-4V
Al 7075
CF/PEEK
    Continuous | Short Carbon Fiber
    +
    PEEK
NEW DESIGN
BASELINE
Notes: In order to cover as much as possible the release or demise of the external panels we focused on a benchmark design composed of …
The addition of an active metallic filler is multiple, it increased the trough thickness thermal conductivity typically lacking in the laminated composite system, while also improving the mx ablation rate by faster matrix pyrolysis.

## Slide 5: Hybrid reinforced composite skin
CF+FF ply-ply hybrid
Evaluation methods
Thermomechanical evaluation | EsaComp, Dynamic mechanical analysis - DMA
  Stiffness/mass ratio: +117% improvement vs Al-2024 | +8% vs CFRP
  Specific Elastic modulus (: +45% vs Al-2024 | +31% vs CFRP
Demise evaluation | TGA, Static reentry chamber with creep loading, PWT
  1%wt AlMg matrix filler integration: → 10-45°C earlier degradation onset (390°C -> 355°C with epoxy)
  → +10-50% degradation rate
  Mechanical failure during static reentry test @ 370°C vs NO failure for CFRP up to 850°C
Flax
Carbon
Carbon
Self-developed static reentry chamber – 100 kW/m2
DMA - 3-point bending setup
Notes: 3 Progressive testing methods
With the 2 first more commercial ones
First is TGA…

## Slide 6: Plasma Wind Tunnel testing
Evaluation methods
CF+FF ply-ply hybrid
CFRP
IRS PWK-4 wind plasma facility
Heat flux – 520 kW/m² | Ambiant pressure 41 Pa
CF+FF hybrid shows
High ablation rate
Faster CF tow erosion
Full ply spallation due to the flax layer
Notes: 3 Progressive testing methods
With the 2 first more commercial ones
First is TGA…

## Slide 7: Short-CF/PEEK fasteners
Thermomechanical evaluation | DMA, tensile, shear testing
  No significant differences in tensile and shear properties between continuous and short CF reinforcement
  Specific tensile failure stress () : +80% vs stainless steel
  Specific shear failure stress (): +295% vs stainless steel
Demise behaviour evaluation | TGA, Static reentry chamber with creep loading
  High heating rate induce higher failure temperature
  Higher strain at fracture with short fiber +30%
  Complete bolt separation with Short-CF design => Allowing panel release !
Evaluation methods
Recovered samples
Static reentry chamber test
Single lap shear setup

## Slide 8
Novel hybrid skin sandwich panel manufacturing
Space qualification test (vibration, TVAC cycling)
What’s next ?
Increase novel assembly design TRL with PWT testing | highest environmental conditions relevancy
Further development of an Experimental-to-Model correlation
Composite fasteners Torque-Load evaluation
Space qualification test (vibration, TVAC cycling)
TRL 3-4 → 5
TRL 2-3 → 5

## Slide 9
Promising composite demise improvement with a combination of carbon and natural fiber (flax) in addition with active metallic filler
An optimal short-CF/PEEK fastener design has been identified by comparative evaluations and relevant testing approaches to replace current critical baselines
Safe and sustainable uncontrolled re-entries can be achieve by selecting and applying efficient material selection and break-up sequence.
Conclusion
Notes: Expectations :
      Fast and early opening of the S/C external panels
        Ideal complete separation from 500°C
      Potential mass budget reduction from its high specific strength
Bolted-joint is a well-known assembly technique
      Facilitated implementation acceptance and procedure

## Slide 10
This work is supported by EPFL and ESA through an NPI program #4000129740/20/NL/MH/hm
Thanks to:
      LPAC team
Acknowledgments
Adam Pagan
Ralf Usigner & Alessando Netti
James Beck
Régis Voilat
Albert Vodermayer
Lionel Metrailler
      Project partners
Notes: I would like to thank my Lab team and all my project partners for their active collaboration and financial support.

## Slide 11: Tank you for your attention !
Any questions ?
Alexandre Looten
Ph.D. student at Swiss Federal Institute of Technology in Lausanne – EPFL
Email: alexandre.looten@epfl.ch
Phone: +41 21 693 48 36

## Slide 12: Annexes

## Slide 13: Demise testing
Thermogravimetry analysis TGA – Thermophysical
  15 µg samples | 40°C/min heating rate | T sweep [30 ; 900]°C | Air or N2 atm | ASTM E1131-20
  Degradation onset temperature | Weight loss rate (T)
Dynamic mechanical analysis DMA – Thermomechanical
  3point bending | 0.1% strain | 10°C/min heating rate | T sweep [-150 ; 350]°C | ASTM D4065-20
  Storage modulus (T) | Melting temperature onset
Evaluation methods
Perkin&Elmer TGA 4000
perkinelmer.com
TA Q800 – 3pt bending setup
Self-designed static reentry chamber with creep load – Thermo-physico-mechanical
  2.9 kN creep preload | Heat flux up to 100 kW/m2 | medium vacuum mbar | 3 high acquisition thermocouples | HD camera
  Full samples demise behaviour
  Mechanical loosening onset (T, t)
  Demise temperature onsets (t)
Notes: 3 Progressive testing methods
With the 2 first more commercial ones
First is TGA…