## Slide 1: In-orbit results from CELESTA
Presenter: Andreas Waets (CERN)
Material prepared by: Raffaello Secondo (CERN) and Andrea Coronetti (CERN)
With input from: Rubén Garciá Alía (CERN), Salvatore Danzeca (CERN), Ivan Slipukhin (CERN), Alessandro Zimmaro (CERN), Paul Peronnard (CERN), Markus Brugger (CERN), Alessandro Masi (CERN), Enrico Chesta (CERN)
Notes: Speaker notes:
[Text]
My notes:

## Slide 2: CELESTA MISSION - BACKGROUND
CERN Latchup Experiment and STudent sAtellite: CELESTA.
The scientific Payload of the first CERN-driven Small Satellite.
Collaboration started in 2014
Content of the Talk:
  Design and test results conducted between 2014 and 2017
  In-Flight data analysis: BE-CEM-EPR, SY-STI-BMI
Test Platform:
CHARM a mixed-field facility.
The RadMon V6:
CERN Radiation Monitoring System
ROBUSTA:
CSUM - 1U CubeSat Structure
Notes: Speaker notes:
[Text]
My notes:

## Slide 3: GOALS
CubeSat Payload version of the CERN RadMon V6.
Nanosatellites radiation qualification procedure at CHARM.
Comparison of radiation effects between LEO space environment and CHARM.
Test the ROBUSTA platform.
ROBUSTA: Radiation On Bipolar
University Satellite Test Application
Notes: Speaker notes:
[Text]
My notes:

## Slide 4: The RadMON
TID Measurement: 100 nm and 400 nm RadFETs.
Displacement Damage: P-i-n Diodes.
HEH and ThN fluence: Two Memory Banks, Cypress and Toshiba SRAM
Based on COTS.
P-i-n diodes
RadFET
Cypress SRAM
Toshiba SRAM
SENSORS
Notes: Speaker notes:
[Text]
My notes:

## Slide 5: Analysis of Mission Environment
Two initial Low Earth Orbits (LEO) proposed:
  Circular: 600 km x 600 km Perigee/Apogee.
  Elliptical 300 km x 1200 km Perigee/Apogee.
  Note: final orbit is different from initial analysis
Simulations: STELA + Omere + CREME.
Events concentration: polar cusps + SAA.
SEU Prediction
TID: 84 Gy.
Total Fluence (HEH>20 MeV): order of 1010 HEH/cm2 for an elliptical orbit
Impact of radiation on a given orbit
STEP 1
Feasibility study – Mission Constraints
STEP 2
3D Model FASTRAD analysis
STEP 3
Prototype Test-Board.
Characterization of sensors and full system at CHARM.
Design of Final Payload.
Notes: Speaker notes:
[Text]
My notes:

## Slide 6: Focused beams and Mixed-Field
CHARM:
Mixed-particle field
Testing at System Level
Representative radiation fields for space proton environment
CHARM: Cern High Energy AcceleRator MixedField/Facility
The PSI-PIF Irradiation Area
PSI:
Focused Mono-energetic proton beam.
COTS Characterization.
Notes: Speaker notes:
[Text]
My notes:

## Slide 7: First Test in a Mixed-Field
Latchup Experiment: Brilliance SRAM BS62LV1600EIP.
UART communication using MODBUS protocol.
COTS selected in terms of TID, SEE and temperature (-20 to 80)
SEU: Cypress SRAM CY62157EV.
FPGA: ProASIC3
Dose: Tyndall RadFet 100 nm.
FIRST PROTOTYPE test board
Notes: Speaker notes:
[Text]
My notes:

## Slide 8: SEL Analysis at PSI on SRAM Candidates
DUT Label | Reference | Manufacturer
SRAM A | IS61LV5128AL-10TLI | Issi
SRAM B | BS62LV1600EIP55 | Brilliance
SRAM C | AS7C34098A-10TNC | Alliance
Candidate SRAM tested
Flux = 6.4·107 p/(cm2·s).
Fluence = 1·1010 p/cm2.
Current threshold: 50 mA for SRAM A and C, 10 mA for SRAM B.
Used different detection systems: LatMon, GUARD, Controlled Power Supply
Latchup Current waveforms: SRAM B lower consumption
Notes: Speaker notes:
[Text]
My notes:

## Slide 9: SEL Results at CHARM - II
SRAM B Lot II - Test Location 4
Flux = 4.6x105 HEH/(cm2 ·s)
SRAM B: 4900 SEL.
Average σ = ~1.3 x 10-8 cm2
Notes: Speaker notes:
[Text]
My notes:

## Slide 10: CELESTA Payload Radiation Qualification - Overview
Mission Analysis and first test on a prototype board
SEL characterization
RadMON TID and SEU/MBU
Analysis
Tests on candidates COTS at PSI (ADC, Voltage regulators, opamps…)
CAN transceiver

## Slide 11: The CELESTA PAYLOAD Module
Weight: 52 g.
Modular: “Mother Board” + Mezzanine.
180 mW average power.
300 mW peak power.
ROBUSTA compatible, CAN compatible.
Mother Board
Fully assembled
Integration on ROBUSTA
Notes: Speaker notes:
[Text]
My notes:

## Slide 12: Test Setup in CHARM
Timings:
  2 min reading of the quantities.
  1 min reading of the SRAMs.
CHARM configurations:
  Copper Target + Full shielding (CIIC)
  Partial Shielding (OOIC)
  No shielding (OOOO)
Notes: Speaker notes:
[Text]
My notes:

## Slide 13: Experimental Results - TID
140 Gy collected during 4 days of irradiation
Notes: Speaker notes:
[Text]
My notes:

## Slide 14: Experimental Results – All sensors
R. Secondo, “Upgrades of the RadMon V6 and its Integration on a Nanosatellite for the Analysis and the Comparative Study of the CHARM and Low Earth Orbit Environments”, PhD Thesis, Université de Montpellier, 2017.
Degradation of SEL cross section with TID (~5 krad)
Notes: Speaker notes:
[Text]
My notes:

## Slide 15: Vega-C Launch – July 2022
13th July 2022 – ESA VEGA-C Inaugural Flight
Notes: Speaker notes:
[Text]
My notes:

## Slide 16: CELESTA orbit and mission
Vega-C maiden flight
Perigee altitude: 5865,4 km
Apogee altitude: 5866,9 km
Inclination angle: 70,16°
Right ascension of the ascending node (RAAN): -52,3°
Argument of perigee: 142,9°
Orbital period: 3.74 hours
Mission launch: 14.07.2022
Data collection starting 20.07.2022
Mission end: 12.09.2022
Trajectory of CELESTA as calculated in OMERE
VEGA-C
Notes: Speaker notes:
[Text]
My notes:

## Slide 17: Flight data summary
347 orbits completed
Results for SELs on two Brilliance units as a function of time
SEU and TID data: RADECS ‘23 paper
No possibility for the geolocalization of the events
Courtesy of
A. Coronetti, R. Garcia Alia,
I. Slipukhin
(CERN, SY-STI-BMI),
S. Danzeca, A. Zimmaro (CERN, BE-CEM-EPR)
Notes: Speaker notes:
[Text]
My notes:

## Slide 18: Flight data against predictions
OMERE 5.4.1 used to calculate the environment for the mission timeframe
Models used: AP8, AE8, ESP, GCR ISO 15390:2004
CHARM HEH cross-section for flight date code
  1.33 x 10-8 cm2
  Step response with E0 = 20 MeV
Weibull response for ions
2 µm sensitive cell depth
Orbiting deep inside proton belt  proton dominance in the response
GCR Heavy ions rate | 0.29 /dev/day
GCR Protons rate | 0.01 /dev/day
Trapped Protons rate | 1.31 /dev/day
Avg Solar Protons rate | 0.01 /dev/day
Total predicted rate PSI+UCL | 1.62 /dev/day
Total rate CHARM | 2.15 /dev/day
Flight rate SEL1 | 1.59 /dev/day
Flight rate SEL2 | 1.22 /dev/day
Courtesy of
A. Coronetti, R. Garcia Alia, I. Slipukhin
(CERN, SY-STI-BMI),
Notes: Speaker notes:
[Text]
My notes:

## Slide 19: Conclusions
First CubeSat Mission collaboration between CSUM and CERN
CELESTA led the way to a procedure to test small satellites at system level
Payload tested in a LEO representative mixed-field.
Good agreement over predicted and in-flight SEL data.
Notes: Speaker notes:
[Text]
My notes:

## Slide 20
Big thanks to all contributors!
CERN BE-CEM-EPR, SY-STI-BMI and the CSU Montpellier

## Slide 21: The CHARM Facility
Representative Environments:
  Target material
  Shieldings
  Test Position
Iron
Concrete
Notes: Speaker notes:
[Text]
My notes:

## Slide 22: Experimental Results – HEH Fluence
SEU count still valid at TID = 386 Gy.
Final HEH flux value 6x1010 HEH/(cm2 ·day). In agreement with the expected flux rates, between 5x1010 and 1x1011 HEH/(cm2 x day).
Final fluence 1x1012 HEH/(cm2 xday): no SEL, no major failures.
R. Secondo et al., "A Nanosatellite Radiation Qualification Procedure At The CHARM Facility Based On The CELESTA Payload Demonstrator", ESA 4S Symposium 2016, Malta, 2016, pp. 1-11.
Notes: Speaker notes:
[Text]
My notes:

## Slide 23: SEL Detection Circuit
Analog components - no ADC.
INA146: TID up to 500 Gy in low gain configuration.
LM124: SEL tolerant, TID up to 500 Gy.
BST82: TID up to 320 Gy.
Qualification at CHARM: monitoring signals and supply currents.
Custom-made SEL board to easily test each component
Oscilloscope
Test in Position 4
Notes: Speaker notes:
[Text]
My notes:

## Slide 24: SEL Results at CHARM - I
Latchup current waveforms.
SRAM A (Issi) and SRAM B (Brilliance)
Example of Latchup signals
R. Secondo et al., "Analysis of SEL on Commercial SRAM Memories and Mixed-Field Characterization of a Latchup Detection Circuit for LEO Space Applications“, in IEEE Transactions on Nuclear Science, vol. 64, no. 8, pp. 2107-2114, Aug. 2017
Notes: Speaker notes:
[Text]
My notes:

## Slide 25: The ROBUSTA Platform
PAYLOAD components:
Packaging: Vibrations + Mass (200 g max).
Mechanical: Board size + Integration in the platform.
Power: < 600 mW average power.
Temperature: -20 ˚C to 80 ˚C.
Communication: CAN Bus
EPS - Electrical Power Subsystem
TT&C - Tracking, Telemetry & Command
OBDH - On Board Data Handling
PL - The Payload
Notes: Speaker notes:
[Text]
My notes: