## Slide 1
MOSFET commercial plastic components survey and its SEE behavior

## Slide 2: TABLE OF CONTENTS
Motivation
MOSFET Structures
OSIP
Selection
Results
Conclusion

## Slide 3: Motivation
New Space missions demands an increasing number of COTS
COTS components may give a performance not available in hi-rel components
Discrete and IC are subject to radiation damage
MOSFET are key in electronics equipments

## Slide 4: MOSFET Structures
LDMOS
Introduced in the 70’s
Higher channel resistance
Not usually suitable for power applications
VDMOS
Can sustain high blocking voltaje and high current
Lower channel resistance compared to LDMOS

## Slide 5: MOSFET Structures
Trench-gate
On resistance decreases importantly
Capable of great power handling
Not designed for high voltages
Superjunction-MOS
Low on-resistance
Vb sensitive to imbalance condition of charge
Designed for high voltages

## Slide 6: OSIP
Open Space Innovation Platform

## Slide 7: Selection
DoEEEt Analytics
Survey
Procurement history

## Slide 8: DoEEEt analytics

## Slide 9: Procurement historic

## Slide 10: Surveys
15 main players of European space industry were contacted
Answers were collected and matched the general trend found previously
General concern about finding MOSFET for New Space/lower grade missions
Baseline Part number | Back-up part number | Back up part number MFR
PMPB85ENEAX (Nexperia) | SQ2362ES-T1_BE3 | Vishay
 | PMN40SNAX | Nexperia
 | RF4L055GNTCR | Rohm
 | BSL606SN H6327 | Infineon
FDD8896 (Onsemi) | PSMN3R4-30PL,127 | Nexperia
 | BSC034N03LSGATMA1 | Infineon
 | PSMN2R5-30YL,115 | Nexperia
 | SI4634DY-T1-GE3 | Vishay
FDC608PZ (Onsemi) | SI3443CDV-T1-GE3/SI3443CDV-T1-BE3 | Vishay
 | SQ2351ES-T1_BE3 | Vishay
 | SI5457DC-T1-GE3 | Vishay
 | PMN42XPEAX | Nexperia

## Slide 11: Summary Results: TEST CONDITIONS
FDD8896 (TRENCH N-MOS) |  | 
Signals | Nominal Voltages | Threshold Currents
VGS | 0 V | IGS= 100 nA
VDS | 5 V 10 V 15 V 20 V 30 V | IDS = 250 uA
PMPB85ENEAX (TRENCH N-MOS) |  | 
VGS | 0 V | IGS= 10 uA
VDS | 10 V 20 V 30 V | IDS = 10 uA
FDC608PZ (TRENCH P-MOS) |  | 
VGS | 0 V | IGS= 10 uA
VDS | -5 V -10 V -15 V -20 V | IDS = 1uA
PROCESS STEPS:
Pre run test: Initial gate stress (No Irradiation)
Pre run test: Functionality device test (No Irradiation)
Run test: exposition under biasing conditions (Irradiation)
Post run test: Post irradiation gate stress (No Irradiation)

## Slide 12: Summary Results: FDD8896 - NMOS
Tested under Effective LET at Surface 16.1 and 32.4 (MeV/mg/cm2) and Fluence 3.0E5 (p/cm2)
No SEGR events were observed
No SEB events were observed
The device is sensitive to heavy ions induced degradations.
Drain leakage increases with irradiation.
Degradation is higher at higher LET and at higher drain voltage.
Degradation is attributed to localized dose deposition in the trenches of the device.

## Slide 13: Summary Results: PMP85ENEAX - NMOS
Tested under Effective LET at Surface 16.1 and 32.4 (MeV/mg/cm2) and Fluence 3.0E5 (p/cm2)
No SEGR events were observed
No SEB events were observed
The device is sensitive to heavy ions induced degradations.
Drain leakage increases with irradiation.
Degradation is higher at higher LET and at higher drain voltage.
Degradation is attributed to localized dose deposition in the trenches of the device.

## Slide 14: Summary Results: FDC608PZ - PMOS
Tested under Effective LET at Surface 32.4 and 62.5 (MeV/mg/cm2)
Fluence 3.0E5 (p/cm2)
No SEGR events were observed
No SEB events were observed
The device is no sensitive to heavy ions induced degradations under 32.4(MeV/mg/cm2).
Increasing of drain and gate leakage currents was observed due to the charge collection under 62.5 (MeV/mg/cm2).

## Slide 15: Summary and future work
The use of commercial and AEC-Q MOSFET will continue.
Results from different sources can build more robust knowledge.
The results show that the use of the commercial trench MOSFET can be evaluated based on the radiation profile of the mission.
Radiation results show dose sensitivity.
More MOSFET structures/technologies and even other components need to be addressed for future missions.

## Slide 16
José Largaespada Gómez: josef.largaespada@altertechnology.com
Fernando Romero Madera: fernando.romero@altertechnology.com
https://www.altertechnology-group.com/es/home/
https://www.doeeet.com/
THANK YOU!