## Slide 1
KREPE-2 Flight: now with spectral data of the stag line!
(to be shown at RHTG 11th)

## Slide 2: Motivation
During hyperbolic planetary entry, spacecraft can attain entry speeds of 10-16 km/s which results in high surface heat fluxes and intense radiation in the shock layer
The heat flux generated by radiative emissions is often on-par with the convective heat flux
It had been previously held that the incoming radiative flux was either reflected at the surface, or absorb within a 1 mm thickness of the surface
Because most TPS are far thicker than the absorption zone, the penetration of radiation within the heat shield is usually neglected
However, a recent experimental study shows that spectral radiation can penetrate the ablator and affect the material response over a significant depth
Because shock layer radiation is dominated by single wavelength emissions, it is thus important to account for it

## Slide 3: Charring ablators
Micrographs of PICA at different magnifications. (Agrawal et al., 2013)
Agrawal, P., Chavez-Garcia, J. F., and Pham, J., “Fracture in Phenolic Impregnated Carbon Ablator,” Journal of Spacecraft and Rockets, Vol. 50, No. 4, July-August 2013.
Charring ablators are made by impregnation of phenolic resin on preform matrix
The material has two “phases”, consisting of a network of carbon fibers and a very porous phenolic matrix dispersed on and in between the fibers
The highly porous structure makes it a low-density material (ablator)

## Slide 4: Laser testing on ablative materials
Experiment conducted by White, comparing ablation behavior after heating ablative samples with a laser, with same irradiance and the same duration, but at different wavelengths
Two laser were used, one at 1.07 μm (Fiber), and the other at 10.6 μm (CO2)
Conventional arc-jet tests cannot produce such results
White, S., “Effects of Laser Wavelength on Ablator Testing,” 38th Annual Conference on Composites, Materials and Structures, Cocoa Beach, Florida, January 2014.

## Slide 5: Experimental results
Results show significant difference in char layer thickness, mass loss, maximum bondline temperature and time to maximum bondline temperature
The shorter the wavelength, the thicker the char and pyrolysis layer
The shorter wave- length results in deeper in-depth absorption
Since the shock layer radiation is wavelength dependent, this needs to be accounted
Picture taken from: White, S., “Effects of Laser Wavelength on Ablator Testing,” 38th Annual Conference on Composites, Materials and Structures, 2014.

## Slide 6: Nomenclature
Pure conduction
Conduction coupled with radiative emission
P1 approximation method
  and

## Slide 7: Material response
Radiative equation added to the the KATS-MR material response code
Dynamically coupled, based on a the change in the temperature field
KATS-MR
  A porous media thermochemical solver for modeling charring and surface ablators
  Able to do thermo-structural coupling
  Resolves the VANS equations
    multi-species mass conservation
    3D full momentum transport
    energy conservation
  Optionally uses stochastic properties for modeling variability and uncertainty
  Newly coupled to several aerothermodynamic CFD codes (US3D, CHAMPS, KATS-FD)

## Slide 8: Verification
Marschall et al. cases

## Slide 9: Verification
Marschall et al. cases
Radiant heating
Arc-jet heating
Shuttle entry

## Slide 10: Verification
2D IsoQ sample

## Slide 11: Verification
2D IsoQ sample

## Slide 12: Verification
2D IsoQ sample

## Slide 13: Charring ablator and lasers
The experiment by White is qualitatively modeled
A 1-in charring ablator is assembled using:
  TACOT (PICA) density and decomposition rates
  LI-900 extinctions/absorption spectral coefficients, heat capacity and gas/solid conductivity
115 W/cm2 heat flux is applied for 30 s to the ablator using:
  surface conductive heat flux
  a 1.07 μm laser
  a 10.6 μm laser
Picture taken from: White, S., “Effects of Laser Wavelength on Ablator Testing,” 38th Annual Conference on Composites, Materials and Structures, 2014.
10.6 μm
1.07 μm

## Slide 14: Charring ablator and lasers
8

## Slide 15: Charring ablator and lasers
Extinction β
Absorption K
Optical coefficients
Laser 1.07 μm
  K = 0.1211 cm-1
  β = 69.85 cm-1
Laser 10.6 μm
  K = 15.18 cm-1
  β = 233.2 cm-1
[1] Marschall, J., Maddren, J., and Parks, J., “Internal Radiation Transport and Effective Thermal Conductivity of Fibrous Ceramic Insulation,” 35th AIAA Thermophysics Conference, Anaheim, CA, June 2001.
Laser 1.07 μm
Laser 10.6 μm

## Slide 16: Charring ablator and lasers

## Slide 17: Charring ablator and lasers
Absorption in material
The 10.6 μm laser are immediately absorbed, within the first mm
The 1.07 μm laser is absorbed throughout the whole material (and even leaves it)

## Slide 18: Charring ablator and lasers
Temperature traces
Temperature histories at both surfaces, and 4 equidistant lengths inside the material
The pure conduction and the 10.6 μm laser results are very similar
The heating from the 1.07 μm micron laser happens from within

## Slide 19: Charring ablator and lasers
Temperature
With the laser, the surface is heated from within, and not directly from the applied heat flux
The effect is much more evident for the 1.07 μm micron laser but still there for the 10.6 μm
Loss through surface emission is reduced
The 10.6 μm laser and the conduction results are nearly identical
The discrepancy is also due to the different conduction models (keff vs ks/g + radiation)
The results confirms the experimental observations: increased bondline temperature and reduced time to bondline

## Slide 20: Charring ablator and lasers
Density
Replicates the behavior observed in White’s experiment
Increased char layer thickness and increased mass loss for the 1.07 μm laser
The conduction has results almost identical to the 10.6 μm laser

## Slide 21: Charring ablator and lasers
Density profile
An increase in density near the surface is observed (or more accurately, a “decrease in density reduction”)
Since absorption is from within, surface heating is mostly done from the inside out, and not from the outer flux, there is.
This phenomenon is routinely observed in flight tests (but not in arc-jet tests!)
Thought to be due to coking (carbon deposition due to pyrolysis gas flow), but maybe it is not…

## Slide 22: Material response to shock-layer radiation
Three types of methodologies exist to solve the radiative transfer equation inside the solids for spectral flux as boundary condition:
  Full Spectrum Resolved Model: the number of equations solved is equal to number of spectral grid points
  Kappa Resolved Model: the number of equations solved is equal to the number of absorption coefficient points
  Band model: the number of equations solved is equal to the number of bands

## Slide 23: Material response to shock-layer radiation
Band Model for LI-900 material
Absorption coefficient
Extinction coefficient

## Slide 24: Material response to shock-layer radiation
Band Model: Verification
Artificial spectrum
Temperature histories for all three models

## Slide 25: Material response to shock-layer radiation
Results

## Slide 26: Material response to shock-layer radiation
Results

## Slide 27: Material response to shock-layer radiation
Results

## Slide 28: Material response to shock-layer radiation
Results

## Slide 29: Conclusion
The verification conducted on multidimensional meshes implies the high robustness of the coupling scheme.
Laser ablation simulations confirm the behavior noticed from the White experiments.
The material response to shock layer radiation show higher internal temperatures and earlier internal de-composition when the spectral part of the radiation is considered.
Acknowledgements
Financial support for this work is provided by NASA SpaceTech-REDDI-2018-ESI grant 80NSSC19K0218
Thanks to A. Brandis for providing the spectrum

## Slide 30
Evaluation of solid plus gas thermal conductivity for fibrous materials
Pure conduction:
Conduction coupled with radiative emission
is numerically calibrated and the values evaluated are dependent on the radiative transfer equation method used.
At steady-state,
Internal radiation
1

## Slide 31
Internal radiation
Preliminary results
For LI-900 material, at p = 1 atm
Calibrated solid plus gas thermal conductivity values
2

## Slide 32: Preliminary results
Pure conduction
Coupling scheme with
Marschall values
Coupling scheme with
present work
Temperatures contours for pure conduction and coupling scheme
Absolute difference in temperatures between pure conduction and coupling scheme

## Slide 33
Preliminary results
Temperatures histories for pure conduction and coupling scheme along stagnation line and shoulder
Absolute difference in temperatures histories between pure conduction and coupling scheme