## Slide 1: Characterization and Measurement of the SET Pulse Duration of the DARE65T Standard Cells Libraries
Laurent Berti

## Slide 2: Outline
Introduction
SET characterization test structure
  Architecture
  Calibration
  Double hit probability
Measurement results
  Cross section INVD1 vs flavor
  Cross section versus drive strength
  SET pulse width distribution
Conclusion

## Slide 3: Introduction
Proper hardening of a digital circuit is related to:
  An error rate specification
  Mission profile, orbits...
Many way to harden a digital circuit
  Best hardening has an important cost in area, power and speed
To predict the error rate and to optimize the level of hardening, we need:
  Cross section versus LET
  Distribution of the SET duration versus LET
The goal of this TV is by measuring the cross section and the SET duration on a limited subset of the standard cells, to be able to calculate them for any standard cells of the DARE65T libraries.

## Slide 4: SET characterization test structure
Victims are a limited subset of the std cells libraries:
  INV D1, D3, D4 & D16
    Gate length of 60nm and 70nm
    Threshold flavor: Low, Standard and High
  CCELL D1, D2 & D4
  Hardened logic: INVBLx, NAND2BLx & NORD2BLx
Victim arranged in chains of 16 or 32 cells:
  Representative of real logic cone
  Not too long chain to avoid an important pulse broadening (~2ps/gate)
  Parallelization of the victims is done thanks to a balanced NAND/NOR combiner
Architecture

## Slide 5: SET characterization test structure
Architecture

## Slide 6: SET characterization test structure
Delay SET filter measurement
  Ring oscillator using same delay elements
  Validation of the pulse distortion with the measurement of well-known pulse width
Calibration

## Slide 7: SET characterization test structure
Target: 100 hits on the victim chains in 15 minutes under a flux of 10k particles/(s*cm2)
  Sensitive area of the victims = 100 / (15 * 60 * 10k) = 1111 µm2
Readout frequency of each test structure output: 100Hz
Each strikes are independent
  Probability to have a double strike during 10 ms
  Average number of measurement with double strike during a period of 15 minutes
Double hit probability

## Slide 8: Measurement results
Cross section INVD1 vs flavor

## Slide 9: Measurement results
Without surprise:
  Saturation cross section similar for the different flavors (Vth and gate length)
  Low LET cross section strongly impacted by the Vth
    LVT drive strength > SVT drive strength > HVT drive strength
  Low LET cross section lightly impacted by the gate length (60 nm vs 70 nm)
Cross section INVD1 vs flavor
LET (MeV.mg-1.cm2) | Cross section (cm2) |  |  |  |  | 
 | HVT60N | HVT70N | SVT60N | SVT70N | LVT60N | LVT70N
7.2 | 2.78E-09 | 2.88E-09 | 2.32E-09 | 2.71E-09 | 1.62E-09 | 1.92E-09
13.3 | 4.59E-09 | 4.39E-09 | 4.37E-09 | 4.39E-09 | 3.69E-09 | 3.98E-09
24.5 | 5.86E-09 | 6.13E-09 | 5.18E-09 | 5.44E-09 | 4.98E-09 | 5.05E-09
33.5 | 8.89E-09 | 8.67E-09 | 7.62E-09 | 8.15E-09 | 7.06E-09 | 7.81E-09
48.5 | 8.35E-09 | 8.64E-09 | 7.79E-09 | 7.96E-09 | 7.20E-09 | 7.30E-09
66.3 | 1.34E-08 | 1.30E-08 | 1.24E-08 | 1.23E-08 | 1.16E-08 | 1.20E-08

## Slide 10: Measurement results
Cross section vs Drive Strength

## Slide 11: Measurement results
LET threshold strongly dependent of the drive strength: proportionality observed
Saturation LET looks similar but... :
  INVD1 has 1 finger and INVD2 has 2 fingers => same junction area but the higher drive strength decrease a little bit the saturation LET
  INVD4 has 4 fingers and the 2 drains are close to each other => less than factor 2 with INVD2
Cross section INVD1 vs Drive Strength
LET (MeV.mg-1.cm2) | Cross section (cm2) |  |  |  |  | 
 | INVD1 |  | INVD2 |  | INVD4 | 
 | SVT60N | LVT60N | SVT60N | LVT60N | SVT60N | LVT60N
7.2 | 2.32E-09 | 1.62E-09 | 1.35E-10 | 0.00E+00 | 0.00E+00 | 0.00E+00
13.3 | 4.37E-09 | 3.69E-09 | 2.37E-09 | 1.08E-09 | 2.96E-10 | 0.00E+00
24.5 | 5.18E-09 | 4.98E-09 | 5.03E-09 | 4.30E-09 | 4.27E-09 | 2.37E-09
33.5 | 7.62E-09 | 7.06E-09 | 6.47E-09 | 5.74E-09 | 7.67E-09 | 4.70E-09
48.5 | 7.79E-09 | 7.20E-09 | 6.88E-09 | 6.93E-09 | 1.04E-08 | 9.81E-09
66.3 | 1.24E-08 | 1.16E-08 | 9.55E-09 | 8.67E-09 | 1.22E-08 | 1.23E-08
S
S
D
S
D
S
S
D
S
S
D
S

## Slide 12: Measurement results
SET pulse width distribution

## Slide 13: Measurement results
SET pulse width distribution

## Slide 14: Measurement results
SET duration is about 100ps to 250ps
  Increase with LET
  Decrease with drive strength
SET pulse width distribution
[4] Zheyi Li, Maxim Gorbunov, Henrique Caldas Kessler, Giancarlo Franciscatto, Venkata Sathyajith Kampati, Jinghao Zhao, Jeffrey Prinzie, Laurent Berti; “A Charge-Width Calibration Approach for the Compact Modeling of Single Event Transients”, RADECS 2025

## Slide 15: Conclusion
Cross section of the inverters of the 6 DARE65T standard cells libraries have been measured accurately
Thanks to the simplicity of the layout of the inverters, these results can be used to calculate the cross section of any other standard cells of these libraries
  Saturation cross section of any of the standard cell of the DARE65T platform can be directly extracted from the layout
  The LET threshold is proportional to the drive strength
  The cross section versus LET of any standard cell can be calculated
The SET duration versus LET has been measured for Drive Strength 1 till Drive Strength 16 => DARE65T striker has been updated accordingly (RADECS2025 paper)
Using these data, it is possible to predict the soft error rate of a given digital circuit.

## Slide 17: Backup slides
[3] Zheyi Li; Laurent Berti; Jan Wouters; Jialei Wang; Paul Leroux, “Characterization of the Total Charge and Time Duration for Single-Event Transient Voltage Pulses in a 65-nm CMOS Technology”, IEEE Transactions on Nuclear Science ( Volume: 69, Issue: 7, July 2022)