## Slide 1: Test System for the Experimental Evaluation of a Low-Power High Performance Four-channel ADC for Space Applications
L. Carranza; M.A. Jalón; J.J. Medina (ALTER Technology Spain)

## Slide 2: ALTER TECHNOLOGY GROUP
At a glance
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 3
  Device Under Test: QUAD-ADC
    4 channels
    Simultaneous sampling
    14-bit @ 80 Msps
    1.8 V power supply
    2 Vpp input signal
    CMOS parallel digital output
    Radiation Hardened by Design (RHBD)
  Test System Architecture
    Designed to measure the converters’ Static and Dynamic parameters automatically.
  Radiation Tests
    Total Ionizing Dose (TID)
    Single Even Effect (SEE)
Outline
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 4: QUAD-ADC Test System Architecture
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 5: QUAD-ADC Test System Architecture
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 6
+Vdd
-Vdd
GND
QUAD ADC
DAQ
Synthetic Signal Generator
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
CHx
CHy
RF TRANSFORMER
ADC DRIVER
RF Signal Relay
Solder
Link
DATA
DRIVER
CH1
DATA
DRIVER
CH2
DATA
DRIVER
CH3
DATA
DRIVER
CH4
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
CLK IN
QUAD
ADC
RF Signal Relay
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
ANALOG
& DIGITAL
DRIVERS PWR
ATE APPLICOS ATX7006
CH2 IN
CH3 IN
PWR SOURCE
VOLTAGE
REFERENCES
AMICSA 2025│ June-2025 │ALTER Technology Spain
QUAD-ADC Test System Architecture

## Slide 7: QUAD-ADC Test System Architecture
+Vdd
-Vdd
GND
QUAD ADC
DAQ
Synthetic Signal Generator
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
CHx
CHy
RF TRANSFORMER
ADC DRIVER
RF Signal Relay
Solder
Link
DATA
DRIVER
CH1
DATA
DRIVER
CH2
DATA
DRIVER
CH3
DATA
DRIVER
CH4
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
CLK IN
QUAD
ADC
RF Signal Relay
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
ANALOG
& DIGITAL
DRIVERS PWR
Low Jitter CLK
ATE APPLICOS ATX7006
CH2 IN
CH3 IN
PWR SOURCE
VOLTAGE
REFERENCES
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 8
SW: C#
Control / DAQ
DATA PROCESSING
+Vdd
-Vdd
GND
QUAD ADC
DAQ
Synthetic Signal Generator
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
CHx
CHy
RF TRANSFORMER
ADC DRIVER
RF Signal Relay
Solder
Link
DATA
DRIVER
CH1
DATA
DRIVER
CH2
DATA
DRIVER
CH3
DATA
DRIVER
CH4
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
CLK IN
QUAD
ADC
RF Signal Relay
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
ANALOG
& DIGITAL
DRIVERS PWR
Low Jitter CLK
ATE APPLICOS ATX7006
CH2 IN
CH3 IN
PWR SOURCE
VOLTAGE
REFERENCES
AMICSA 2025│ June-2025 │ALTER Technology Spain
QUAD-ADC Test System Architecture

## Slide 9
Low Jitter CLK
Filter
CLK distribution system
FPGA Single Board Module
APPLICOS ATE
QUAD-ADC Test PCB
PWR Sources
AMICSA 2025│ June-2025 │ALTER Technology Spain
QUAD-ADC Test System Architecture

## Slide 10
TID radiation PCB with samples
QADC performance measurement PCB
AMICSA 2025│ June-2025 │ALTER Technology Spain
QUAD-ADC Test System Architecture

## Slide 11: QUAD-ADC TID: Radiation and measurements results
  TID radiation conditions
  100krad cumulative dose (Cobalt60 source) :
    Dose rate of 210 rad(Si)/h
    Six exposure steps
  Annealing
    24h at 25ºC
    168h at 100º C
  Evaluation of the performance of the QUAD-ADC
  Static parameters: INL, DNL
  Dynamic parameters: SNR, THD, SINA, ENOB, SFDR
AMICSA 2025│ June-2025 │ALTER Technology Spain
  Results
  The static and dynamic performance of the converter was not significantly affected by the TID irradiation.
  The power consumption of the converter remained constant.

## Slide 12: QUAD-ADC SEE Test System Architecture
SW: C#
Control / DAQ
DATA PROCESSING
QUAD ADC
DAQ
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
QUAD
ADC
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
Low Jitter CLK
CH2 IN
CH3 IN
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 13: QUAD-ADC SEE Test System Architecture
SW: C#
Control / DAQ
DATA PROCESSING
+Vdd
-Vdd
GND
QUAD ADC
DAQ
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
QUAD
ADC
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
Low Jitter CLK
CH2 IN
CH3 IN
PWR SOURCE
Analog Signal
Output Circuitry
Latch-Up Detector CTRL & Handler
Main Oscillator
FPGA
ATN SEE TEST SYSTEM
Latch-Up Detector Circuitry
Digital Signal
Generator
UARTs
Interrupt Lines
USB
CTRL Unit
CMD Processor
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 14: QUAD-ADC SEE Test System Architecture
SW: C#
Control / DAQ
DATA PROCESSING
+Vdd
-Vdd
GND
QUAD ADC
DAQ
SET/SEU (ORC) Detector
200 MHz CLK
XEM7350
DDR3 SDRAM
512 MB
UART
Controller
FIFOs
USB Endpoints
FMC Expansion Connector
Kintex-7 FPGA
SDRAM Controller
200 MHz CLK
USB3.0 Link Microcontroller
FMC Expansion Connector
QUAD ADC
Test PCB
CH1 IN
CH1 OUT
CH2 OUT
CH4 IN
CH3 OUT
CH4 OUT
CLK IN
QUAD
ADC
QUAD ADC
OPTIONAL PWR
QUAD ADC
MAIN PWR
Low Jitter CLK
CH2 IN
CH3 IN
PWR SOURCE
Analog Signal
Output Circuitry
Latch-Up Detector CTRL & Handler
Main Oscillator
FPGA
ATN SEE TEST SYSTEM
Latch-Up Detector Circuitry
Digital Signal
Generator
UARTs
Interrupt Lines
USB
CTRL Unit
CMD Processor
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 15: QUAD-ADC SEE Test System
SEE test system inside the radiation chamber: general view
SEE test system inside the radiation chamber: main PCB
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 16: QUAD-ADC SEE Test: Conclusions
Three samples of the converter were irradiated with heavy ions, with energies up to 62.5 MeV.cm².mg-1, while monitoring its operation with the SEE test platform. From the experimental results of high energy ion irradiation on the QUAD-ADC it can be stated that:
  The ADC1480 is immune to SELs up to at least a LET of 62.5 MeV·cm2/mg.
  When the device is exposed to radiation, the consumptions on the analogue and digital sides remain unchanged within their nominal values up to at least a LET of 62.5 MeV·cm2/mg.
  The converter remains functional, i.e. no SEFI has been observed, up to at least a LET of 62.5 MeV·cm2/mg.
  ADC transient Out Of Range Conversions occur from a LET of 46.1 MeV·cm2/mg.
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 17: QUAD-ADC Radiation Test: Conclusions
This work presented the development of a test system designed to evaluate the static and dynamic performance of a prototype four-channel, 14-bit 80 MSPS RHBD. This system has been used to evaluate the radiation resistance of the device.
The integration of the device into a test platform for SEE characterization has been also presented, along with results demonstrating the ADC's resistance to radiation.
The results of the TID tests show that no significant degradations of the static and dynamic parameters are observed. On the other hand, the results of the SEE tests show that the converter is immune to SELs up to at least a LET of 62.5 MeV·cm2/mg and only transient Out of Range Conversions occur from a LET of 46.1 MeV·cm2/mg.
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 18: QUAD-ADC Radiation Test: Acknoledgement
AMICSA 2025│ June-2025 │ALTER Technology Spain
Hugo Serra, Fábio Passos, Edgar Albuquerque, Nuno Paulino, Luís B. Oliveira, João P. Oliveira, Paulo Santos, João Goes
Boris Glass, Sven Wittig
Juan Jose Esteban
Szymon Bednarski (ALTER UK)

## Slide 19
19
19
19
THANK YOU!
AMICSA 2025│ June-2025 │ALTER Technology Spain

## Slide 20: Inspired by knowledge
Juan Jose MEDINA DEL BARRIO Project Lead manager Technical Project Office Department ALTER TECHNOLOGY TÜV NORD S.A.U. Email: jj.medina@altertechnology.com Ph: +34 664 709 958 - mobile Web: www.altertechnology.com Address: C/ Tomás A. Edison 4 41092 Sevilla - SPAIN
Manuel MORALES DOMINGUEZ EEE Parts Engineer and Product Assurance Parts Engineering Department ALTER TECHNOLOGY TÜV NORD S.A.U. Email: manuel.morales@altertechnology.com Ph: +34 673 509 405 - mobile Web: www.altertechnology.com Address: C/ Tomás A. Edison 4 41092 Sevilla – SPAIN