## Slide 1: Demisable Krypton Tank – Final Presentation
Clean Space Days
ESTEC – 30.06.2026

## Slide 2
About Peak Technology
Project Overview
Development Progress
Summary and Outlook

## Slide 3: About Peak Technology
01

## Slide 4: Peak Technology at a glance
CORE COMPETENCE
Ultra-light, high-precision components — produced with Formula 1 development speed and space-grade reliability, powered by fully in-house production and a relentless passion for excellence.
Vienna
Linz
Holzhausen
Wels
Cost
TIME
Quality
LOCATION
Holzhausen, Austria
Team
150 employees

## Slide 5: COPVs FOR SPACE APPLICATIONS
Composite Overwrapped Pressure Vessels (COPV) for Spacecraft and Launchers:
Electric propulsion storage
Propellant tank pressurization
175 L Xenon COPV
30+
40 L Helium COPVs

## Slide 6: Project Overview
02

## Slide 7: Project Overview
Title | Demisable Krypton Tank
Objective | Design and test of a fully demisable krypton tank
Program | ESA ARTES 4.0 CORE COMPETITIVENESS GENERIC PROGRAMME LINE Activity Reference 4B.177 Component A: ADVANCED TECHNOLOGY
ESA Contract No. | 4000143280/24/NL/GM/lf
ESA Technical Officer | Dénis Neves
Project Start | 03/24
Project Closed | 05/26

## Slide 8: Project Overview
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept
Demisable CFRP
Previous Project:
Material development & definition

## Slide 9: Development Progress
03

## Slide 10: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 11: Proof of Concept
Plasma Wind Tunnel test campaign
Samples > Tubes
Results
  CFRP layer fully demised after ~ 2 min
  Proof of concept successful
D = 50 mm
t(CFRP) = 3 mm
t(Aluminium) = 1.5 mm

## Slide 12: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 13: Baseline overwrap design
FEM analysis standard CFRP > not demisable
Requirements
  MEOP (Maximum Expected Operating Pressure): 310 bar
  Pressure safety factors: Proof 1.25xMEOP, Burst 1.5xMEOP
Results
  Standard CFRP layup
  CFRP thickness: 1.88 mm
Liner
Material: aluminium
Volume: 1 L
Outer diameter: 90 mm

## Slide 14: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 15: Mechanical testing Demisable CFRP
Input for demisable overwrap design
Tailored test method
  Longitudinal tensile properties
Results
  Demisable CFRP strain at break ~14 % lower
  Knock-down factor for tensile strength derived

## Slide 16: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 17: Demisable Overwrap Design
 | Overwrap thickness [mm]
Baseline overwrap design | 1.88
Demisable overwrap design | 2.82 (+50 %)
Re-design of baseline
Requirements equivalent
Demisable CFRP based on mechanical testing
Results:

## Slide 18: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 19: Plasma Wind Tunnel Test Campaign
Test on component level
Sample
  1 L COPV
  CFRP thickness: 1.5 mm
  Demisable vs standard CFRP
Rotation to simulate tumbling
Heat flux on sample: 300 kW/m²
Extensive test matrix

## Slide 20: Plasma Wind Tunnel Test Campaign

## Slide 21: Plasma Wind Tunnel Test Campaign
Demisable CFRP
  85 s until full demise
  Short time for full demise (low heat flux!)
  For higher heat flux even ‹60 s
Standard CFRP
  Test stopped after 180 s
  No degradation

## Slide 22: Project logic
Baseline Overwrap Design
Standard CFRP
Mechanical Testing
Demisable CFRP
Plasma Wind Tunnel Testing
Demisable Overwrap Design
Re-entry Simulation
Proof of Concept –
Demisable CFRP

## Slide 23: Re-entry Simulation
Re-entry simulation 1 L COPV
  CFRP thickness 3 mm
  Re-entry tool SAMj by Belstead
Results:
Conclusion:
  COPV can demise during re-entry if it is released at a sufficiently high altitude
Case | Demisable CFRP | Standard CFRP
Full demise | For release altitude ›84 km considering median of all cases | No full demise

## Slide 24: Summary and Outlook
04

## Slide 25: Summary
Demisable 1 L COPV!
Extensive comparison demisable vs standard COPV
Project DEMISABLE KRYPTON TANK successfully closed

## Slide 26: Outlook
Follow up project ZERO DEBRIS PLATFORM
Planned start summer 2026
Development of demisable COPV  TRL 6
COPV volume ~10 L
DRACO project
Project ongoing
Experimental mission  Real re-entry
Demisable & standard COPV

## Slide 27
Technologieparkstr. 6
4615 Holzhausen
Austria, Europe
www.peaktechnology.at
Simone Hartl
Material & Process Engineer
simone.hartl@peaktechnology.at
+43 664 88847186